## Slide 1
Substrate and Gate Current
Channel carrier (electron / hole) heating due to high lateral field (NMOS / PMOS)
Impact ionization  electron / hole pair generation
Substrate current  hole (NMOS), electron (PMOS)
Gate current  Electron or hole injection
D
S
G
B
Non-zero VG and VD
Observed in SiO2, SiON and HKMG technology, in both NMOS and PMOS

## Slide 2
Substrate Current (Hot Carrier)
NMOS
Substrate current:
(1) Increases with VG
(2) Peaks at VG ~ VD/2
(3) Falls for VG > VD/2
Heremans, TED 1988

## Slide 3
Explanation of VG Dependence of ISUB
ID increases with VG
M reduces with VG
DL
N+ poly-Si
N+
N+

## Slide 4
Gate Current (Hot Carrier)
NMOS, Gate Current
Electron injection for VG > VD/2
Hole injection for VG < VD/2
Negligible at VG ~ VD/2 (Due to injection of both electrons and holes)
Hofmann, TED 1985
Hole
Electron

## Slide 5
Explanation of VG Dependence of IG
Lower VG, high M for impact ionization (carrier heating), low ID, negative vertical field near drain favors hole injection
Higher VG, low M for impact ionization (carrier heating), high ID, positive vertical field near drain favors electron injection
D
S
G
B
S
D
Surface potential
Low VG
High VG

## Slide 6
Hole and Electron Injection
Negative vertical field
Positive vertical field
Hofmann, TED 1985

## Slide 7
Summary: Substrate and Gate Current
Impact ionization peaks, co injection of holes and electrons
Vertical field is positive near Drain, electron injection, drops at higher VG due to lower ELAT
Vertical field is negative near Drain, hole injection, drops at lower VG due to lower ID
Hofmann, TED 1985

## Slide 8
Hot Carrier Degradation
Observed in SiO2, SiON and HKMG technology  Degradation of channel/oxide interface and oxide bulk
Observed in both NMOS (negative charge) and PMOS (positive charge)
Localized (near drain) degradation  Shift in VT and gm
D
S
G
B
D
S
G
B
Non-zero VG and VD
Degradation of drain current

## Slide 9
Time Evolution of Degradation
Shift in drain current due to generated interface traps (evidence from charge pumping)
Ang, MR 1999
Lifetime: To reach a given degradation level

## Slide 10
Parametric Shift
Linear correlation between DVT, DSS, Dgm  Interface traps (another evidence)
Hu, TED 1985

## Slide 11
Location of HCD
D
S
G
B
Stress  VG and VD (physical / actual drain)
Forward read  VD at actual drain, damage near actual drain
Reverse read  VD at actual source, damage near electrical source, more impact
Koyanagi, TED 1987

## Slide 12
“Universality” of HCD Time Kinetics
Universal relation when time dependence at different stress conditions is shifted along the time axis
Goo, SSE 1995

## Slide 13
Universal “Universality”
Unique physics governing time kinetics (not understood!)
Mahapatra, TED 2018
Planar and FinFET devices, different channel length, different range of VD

## Slide 14
“Classical” Hot Carrier Mechanism
Maximum degradation coincides with peak ISUB
Hu, TED 1985

## Slide 15
Lucky Electron Model
NMOS: Channel electrons gain energy from drain bias; one of the following happens:
Impact ionization  ISUB
Some electrons scatter towards oxide and get injected  IG
These electrons can also break H passivated defects  NIT
D
S
G
B
Hu, TED 1985
Driven by peak lateral field near drain junction

## Slide 16
Lucky Electron Model
Barrier for I/I
Peak E-field
HC mean free path
Electron injection barrier
Trap generation barrier
Lifetime
Time exponent of HCD
Channel width
Hu, TED 1985

## Slide 17
Failure of Lucky Electron Model
LEM cannot explain VG dependence of lifetime (time to fail) for experiments over wide range of VG
TTF ~ 1/ fixed time degradation
Guerin, TDMR 2007
Data
LEM

## Slide 18
Channel Length Dependence
TTF ~ 1 / fixed time degradation
Non monotonic “U” shaped VG dependence at higher L
Monotonic VG dependence at lower L

## Slide 19
Key Experimental Signatures
Difference in VG dependence for high L, high VD and low L, low VD experiments
Higher degradation with reverse VB, larger impact for larger L
Reverse read more sensitive
Degradation at fixed time
Bravaix, IRPS 2009

## Slide 20
Channel Hot Electron (CHE)
Channel electrons are heated by lateral field
Some hot electrons undergo “re-directional” collision and move towards the interface and create damage
S
D
G
B
High VD
High VG

## Slide 21
CHE: Hot Electron Generation
LG=0.26mm, VFG=6V, VD=3.7V; Electron energy > 3.1eV
HED simulation from SMC
PhD thesis: Deelep Nair, IIT Bombay
S
D
G
B
High VD
High VG

## Slide 22
CHannel Initiated Secondary ELectron
S
D
G
B
M1
M2
Channel hot electrons create primary EHP by M1
Holes flow to bulk, create secondary EHP by M2
Secondary electrons move towards the interface
Electrons create damage near drain
VB <0
High VD
High VG

## Slide 23
CHISEL: Hot Electron Generation
LG=0.26mm, VFG=6V, VD=3.7V; Electron energy > 3.1eV
Broader Damage Area
HED simulation from SMC
PhD thesis: Deelep Nair, IIT Bombay
S
D
G
B
High VG
High VD

## Slide 24
HE Distribution (1D cut along channel)
Broader HED for CHISEL compared to CHE
PhD thesis: Deelep Nair, IIT Bombay

## Slide 25
Electron Energy Distribution
Simulated at maximum injection point at the interface
CHISEL offers energetically higher electron energy distribution
PhD thesis: Deelep Nair, IIT Bombay

## Slide 26
Energy Driven Model
Lateral field induced heating of channel carriers near drain end
Impact ionization and interface trap generation caused by carrier energy
Carrier energy ~ electric field when VD is very high and LEM would work
Electron-electron scattering plays important role when VD is relatively small, and LEM would not work

## Slide 27
Energy Driven Model
Electron energy distribution: f(E)
Impact ionization cross section: SII (E)
Trap generation cross section: SIT (E)
Rauch, TDMR 2005
Guerin, TDMR 2007
Impact ionization rate
Trap generation rate
More work needed to model HCD